## Slide 1
Quantification of the carbonation rate in an embankment after 34 years

## Slide 2: Soil improvement with quicklime Quantification of the carbonation rate in an embankment after 34 years
S. Haas, S. Hammerschmidt (Institute of lime and mortar research, Germany)
A. Shtiza (Industrial Minerals Association Europe, IMA-Europe, Belgium) Ch. Denayer (Carmeuse, Belgium) D. Scutt (Singleton Birch, United Kingdom)

## Slide 3
Facts
Motorway A3 in South-Germany
Built in 1979
Embankment 10 m high
Built in layers
Soil treatment with lime
Varying lime dosages
Quantification of the carbonation rate in an embankment after 34 years
Wikipedia, © BY 2.5
Source : BVK

## Slide 4
Initial Situation 1979
Soil improvement with quicklime
Soil:
  Soft silt
  Water-bearing sands
  Coal-bearing clay
Embankment:
  200.000 m³ excavated silt
  > 20 % (w/w) water content
  ~ 2.5 % (w/w) Calcium-oxide
  8500 t quicklime (CL 90 Q)
Source : BVK

## Slide 5
Drilling site
Sampling
    1990 (11 years)
    2013 (34 years)
Both studies
    Compressive strength
    Water content
2013 study
    Chemical analyses
Soil improvement with quicklime
Drilling site 1990 & 2013
Source : BVK

## Slide 6
Embankment
Soil improvement with quicklime
Source : BVK

## Slide 7
Sampling
Soil improvement with quicklime
Source : BVK

## Slide 8
Reactions : problem statement
Soil improvement with quicklime
Clay
CO2
Ca(OH)2
CSH
CaCO3
CaO
Distribution?
Puzzolanic reactions
Carbonation
Source : BVK

## Slide 9
Reaction quantification (mean values)
Soil improvement with quicklime
Source : BVK
Chart: 
| Available lime | Puzzolanic reaction | Carbonation
 | 0.14 | 0.46 | 0.4

## Slide 10
Based on Best-Available-Technique
Carbon footprint of quick lime – CL90Q
Source: Carmeuse estimate – based of PFR-kilns – CL90Q-high purity
Soil improvement with quicklime
Life Cycle Inventory
LCI EuLA2015 = 1.170 kg/T
  Peer Review
  Downloadable @ GABI
  New LCI under construction
Carbonation rate
40% EuLA – S.Haas & All = 0.314 kg/T
LCI CL90-Q soil stab = 0.856 kg/T
Check the numbers

## Slide 11
Initiatives on-going : Net Zero Carbon Industry by 2050
Soil improvement with quicklime
Chart: 
 | 856 | 500 | -314
2022
2030
2050
CO2/T lime
Source: Carmeuse estimate – own assumptions
A lot of initiatives on-going on …
Carbon Capture Utilization
Carbon Capture Storage
Check the numbers